Hall C Target Configuration

For Gep Jan 2008

David Meekins

January 3, 2008

# Target Positions

The following table gives a list of target positions and materials.  (Listed BDS positions are pre corrections for cryo and vacuum motion).  The home position will NOT remove the entire target stack from the beam.  The configuration is valid from 1/2/08 to 1/30/08.

# Vacuum and Cryo Motion

The vacuum and cryo motion for the target was measured in aggregate.  There were two complete vacuum and cryo cycles before the final number was measured.  This should be the total motion after the survey.  The following table gives the recorded total motion after the survey on 10/24/07

| Scope | Total motion (mm) |
| --- | --- |
| Beam Left Scope | 1.5 up |
|  | 3.4 beam left |
| Beam Right Scope | 1.1 up |
|  | 1.2 beam left |

# Solid Target Ladder

The following table gives the target foil position, thicknesses and chemical purities.

| Target Position | Target | Purity | Thickness g/cm2 |
| --- | --- | --- | --- |
| Empty | n/a | n/a | n/a |
| BeO | Ta | 99.0% | 0.2918 ± 0.0003 |
| Copper | Copper | 99.95% | 0.17775 ± 0.00015 |
| Thin Carbon | Carbon | 99.95% | 0.8879 ± 0.0010 |
| Thick Carbon | Carbon | 99.95% | 2.6547 ± 0.0017 |

Error in thickness is from measurement of area and mass only.  Outside thickness (measured with micrometers) variations in the foils are less than the reported error.  Error also does not include possible voids in materials.

Fluid Targets

There are three loops, each with two cells, on the current cryotarget stack.  The loop 1 is configured with 20 and 15 cm conflat style cells.  Loops 2 and 3 are configured with a new helicoflex style gasket on the exit window side of the block.  The upper cell on each helicoflex block is 4 cm and the lower cell is 20 cm.  The 20 cm cell is offset 38.39 mm downstream to accommodate large angle scattering.  The following table give the cell and radiator thicknesses for each position on the stack.  All cells are made of Al 7075-T6 aluminum alloy.  The 4 cm conflat flange was installed after the initial cool down produced a leak in loop 3.  The original 15 cm cell with radiator in the bottom spot was removed but was reinstalled on Jan 2, 2008.

| Target Position | Entrance window thickness (mm) | Exit window thickness (mm) | Wall thickness (mm) | Radiator Thickness (g/cm^2) |
| --- | --- | --- | --- | --- |
| Loop 1 top 20 cm | 0.122 ± 0.005 | 0.163 ± 0.012 | 0.157 ± 0.017 | n/a |
| Loop 1 bottom 15 cm | 0.117 ± 0.003 | 0.118 ± 0.008 | 0.118 ± 0.008 | 1.123 ± 0.001 |
| Loop 2 top 4 cm | 0.133 ± 0.009 | 0.153 ± 0.009 | 0.145 ± 0.011 | n/a |
| Loop 2 bottom 20 cm | 0.138 ± 0.008 | 0.104 ± 0.009 | 0.138 ± 0.014 | n/a |
| Loop 3 top 4 cm | 0.115 ± 0.008 | 0.142 ± 0.010 | 0.146 ± 0.011 | n/a |
| Loop 3 bottom 20 cm | 0.136 ± 0.008 | 0.130 ± 0.009 | 0.150 ± 0.011 | n/a |

Optics Targets

The optics target has 3 positions.  The first position has 3 foils on each at z = ± 7.5 cm and 0; the second has positions at z = ± 2 cm; the third has positions at z = ± 3.8 cm.  The following table gives the foil thickness and positions.  Carbon foils are 99.95% carbon.  Positions less than 0 are upstream from the nominal target center.

| Position | Z position | Material | Thickness (g/cm2) |
| --- | --- | --- | --- |
| 3 foil | Z = -7.5 cm | Al 6061-T6 | 0.2651 ± 0.0020 |
| 3 foil | Z=0 | Al 6061-T6 | 0.2658 ± 0.0020 |
| 3 foil | Z = 7.5 cm | Al 6061-T6 | 0.2672 ± 0.0020 |
| 2 foil z = ± 2 | z = + 2 | Carbon | 0.1659 ± 0.0012 |
| 2 foil z = ± 2 | z = +-2 | Carbon | 0.1654 ± 0.0012 |
| 2 foil z = ± 3.8 | z = +-3.8 | Al 6061-T6 | 0.2663 ± 0.0020 |
| 2 foil z = ± 3.8 | z = +-3.8 | Al 6061-T6 | 0.2600 ± 0.0019 |

Each of these targets is 25 mm wide at the beam interaction point.  Please see picture to get a better view of the configuration.

Dummy Targets

The dummy targets consists of 2 aluminum alloy foils aligned with the end caps of a given cell (i.e. the 15 cm dummy has two foils placed at z =  ± 7.5 cm).  The foils are 0.8 cm wide (beam transport x direction).  The following table gives the positions and thicknesses of these foils.  The alloy is Al6061-T6.

| Target | Foil Number | Position | Thickness (g/cm2) |
| --- | --- | --- | --- |
| 15 cm Dummy | Foil 1 | Upstream foil | 0.2658 ± 0.0035 |
|  | Foil 2 | Downstream foil | 0.2549 ± 0.0034 |
| 20 cm Dummy | Foil 3 | Upstream foil | 0.2628 ± 0.0035 |
|  | Foil 4 | Downstream Foil | 0.2650 ± 0.0035 |

Pictures