| Element: | WT% |
| --- | --- |
| AlK | 6.02 |
| S K | 1.24 |
| ClK | 3.66 |
| CrK | 19.39 |
| MnK | 0.28 |
| FeK | 64.56 |
| NiK | 4.85 |

# Text boxes

## 304 Sample Deeper Inside Corrosion Pit

## 304 Sample

## 304 Sample at Corrosion Pit

## 304 Sample At Solder Joint