Ceramic Heater Test #1

Heater		Ion Pump	Pyrometer

8 Amps	>2 mA

10.5 Amps	250 uA		581 C

0.0 Amps	30 uA

+1 Day		200 nA

Activation Checkout

Cs 5.0 Amps => >100 uA vacuum burp, quick recovery to 1 uA

NF3 Valve => 1.25 Turns initial response on UHV supply

Ceramic Heater Test #2

10.5 Amps	140 uA		583 C

Vary emissivity at equilibrium - OK

  - 586 C

  - 583 C

  - 578 C

Vary iris at equilibrium – varies, like BP test

Full	582 C

¾	582 C

½	582 C

¼	551 C

1/8	485 C

Using TN for BP calibration to set GaAs=580 C

- pyro vs. thermocouple

- frosting vs. thermocouple

=> *estimate only*	open=650 C & ¼ = 600 C

11.4 Amps	380 uA		630 C

First Activation

- used green light => immediate photocurrent => odd Cs response (5.0 to 4.5 Amps)

- change to 773 nm => usual Cs response => unusual NF3 response => bad lifetime

c)   current depended on EEL bias strongly & BP bias weakly

Ceramic Heater Test #3

11.3 Amps	220 uA		632 C

Second Activation

Today

To-Do’s

- Thermocouple to know RT.

- Thermocouple for calibration against ?

- Absolute calibration of thermocouple & pyrometer by frosting method.

- Laser beam through cesiator.

- Top flange mount for laser, ND’s, camera

- Determine cesiator location

- Possibly change cesiator bellows

- Mask “self-locator”

- EEL battery bias maint.

- EEL picoammeter program/computer needs help