| Date | PR# PO# | Quote# | Qty. | ID# | Remarks | Pieces left? Full square + shard with ~ 5mm active area | Dimensions |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 11-07-03 | PR 215967 PO 03-P1920 |  | 5 | SVT 4577 No name Chip #3 Rudolph Chip #2 Brie Chip #6 5 mm cup SVT 4578 Nougat Chip #3 SVT 4721 Gruyere Chip #3 Gun 3 Chip #2 SVT 4722 Reblochon Chip #3 5 mm cup SVT 4724 | Unanodized, no H dose QE=1% at 780 nm (10-7) P=80% @ 780 nm AP~3% at 780 nm QE killed by H dose SCL seen & gets worse with subsequent heat/clean Anodized by Matt&Marcy QE=0.8% at 780 nm (12-09) P=80% @ 780 nm AP~3% at 780 nm Same as unanodized QE=1.1% at 780 nm (04-01) P~85% at 780 nm 30 min H drops QE and P Loaded #3 in Vgun (1-15) QE=0.6% at 780 nm (high pressure bake) P=75-85% @ 780 nm (QE too low =>bad Mott) Loaded #3 in Vgun (1-27) QE=0.6% at 780 nm (leak) P=80% @ 780 nm 18 min H drops QE and P, but leak: disregard results Loaded in Gun 3, 03-08-04, unanodized, large Ta cup QE=0.4% at 780 nm P~85% at 780 nm (Compton&Mott) Loaded #3 in Vgun (2-10) 5 mm Ta cup QE=1.1% at 780 nm P=80% @ 780 nm Extensive FE test w/ small cup 30 min H drops QE and P Untested, undiced | 0 + 2 1+0 3+3 2+3 All wafer is left | 2” dia. |

SVT Associates:

Contact: Jane Marks (1-952-934-2100)

# Text boxes

4

3

11

12

5

6

7

8

9

10

2

1