## Slide 1
Status and Future Plans for the
SRF Gun at ELBE
FLS2012 ICFA Workshop on Future Light Sources
March 5-9, 2012, Thomas Jefferson Lab, Newport News, VA
J. Teichert (HZDR)
A. Arnold, U. Lehnert, P. Michel, P. Murcek, R. Xiang (HZDR)
T. Kamps, J. Rudolph(HZB)
P. Kneisel (Jlab)
I.Will (MBI)

## Slide 2
1. INTRODUCTION
2. STATUS
- Superconducting Cavity
- SRF Gun at ELBE
- SRF Gun Beam Parameters
- Cs2Te Photo Cathodes
- Multipacting at Cathodes
- Injection in ELBE
3. FUTURE
- New Cavities with High Gradient
- Cryomodule with SC Solenoid
- UV laser for 13 MHz and 500 kHz
OUTLINE

## Slide 3
INTRODUCTION – SRF gun for the ELBE CW Accelerator
Application
high peak current operation for CW-IR-FELs with 13 MHz, 80 pC
high bunch charge (1 nC), low rep-rate (<1 MHz) for pulsed neutron and positron beam production (ToF experiments)
low emittance, medium charge (100 pC) with short pulses for THz-radiation and x-rays by inverse Compton backscattering
Design
medium average current:
1 - 2 mA (< 10 mA)
high rep-rate:
500 kHz, 13 MHz and higher
low and high bunch charge:
80 pC - 1 nC
low transverse emittance:
1 - 3 mm mrad
high energy:
≤ 9 MeV, 3½ cells (stand alone)
highly compatible with ELBE cryomodule (LLRF, high power RF, RF couplers, etc.)
LN2-cooled, exchangeable high-QE photo cathode

## Slide 4
 | Eacc | Epeak on Axis | Ekin
CW | 6.5 MV/m | 17.5 MV/m | 3.3 MeV
Pulsed RF | 8 MV/m | 22 MV/m | 4.0 MeV
measured Q0 is 10 times lower than in vertical test
→ cavity pollution during string assembly?
Maximum achievable field 1/3 of the design value 50 MV/m)
Cavity performance limited by FE & He consumption
Good News
No Q degradation seen since 4 years of operation!
Same performance of cavity with or w/o cathode!
Q vs. E measurement to identify cavity contamination
Summary:
STATUS – Superconducting Cavity
Notes: Lets come to the Q vs. E measurement, as an important instrument to identify cavity contamination!
Measurement done by using this two formulas several times during the last 4 years
A part of them is shown on the left
What we see is measured Q0 is 10 times lower than in vertical test and the maximum achievable field 1/3 of the design value 50 MV/m)
Cavity performance limited by FE & He consumption
But the Good News
No Q degradation seen since 4 years of operation!
Same performance of cavity with or w/o cathode!

## Slide 5
ELBE Superconducting RF Photoinjector
New Injector for the ELBE SC Linac
Test Bench for SRF Gun R&D
STATUS – SRF Gun at ELBE
Dogleg to ELBE
Diagnostic beamline

## Slide 6
STATUS – SRF Gun Diagnostic Beamline
ELBE
Faraday cup: current, bunch charge, dark current
five screen stations with YAGs and OTRs
180° bending magnet: energy and energy spread
transverse emittance: solenoid, quadrupoles, slit mask
Cerenkov radiation station: bunch length
Integrated current transformer (ICT): current, stability
Beam loss monitors
Designed and built by HZB

## Slide 7
t
eEz(t)
RF wave
STATUS – SRF Gun Beam Parameters
Phase scan - low bunch charge
Phase scan - higher bunch charge
bunch charge limit due to space charge

## Slide 8
STATUS – SRF Gun Beam Parameters
Energy and energy spread measurements with 180° dipole

## Slide 9
Transverse emittance with solenoid and quad Scan
slit mask not useable because design is for 9 MeV
improved setup needed!
solenoid for
emittance compensation
field precisely measured
screen DV01
screen DV02
Good agreement with ASTRA
measured normalized emittance 3±1 mm mrad @ 77 pC
Good enough for ELBE injection
STATUS – SRF Gun Beam Parameters
Notes: We also used the diagnostic beamline to measure transverse emittance
Unfortunately slit mask not useable because design is for 9 MeV
We have to use solenoid and quad scan method using solenoid
For this purpose we focus the beam to the first or second screen and calculate the emittance
The result of course is not good but as expected from calculation
Nevertheless operation at 77pC (standard ELBE bunch charge is possible)

## Slide 10
Inside preparation chamber
Cathodes mech. polished and cleaned with Ar+
Heated to 120° C and evaporated with Cs and Te (successive- or simultaneously)
Online thickness and QE measurement
After prep. also QE distribution scan
Vacuum requirement: ~10-9 mbar
STATUS – Cs2Te photo cathodes
Notes: 10
Lets come to the cathode
The preparation chamber consists of two thickness monitors to measure the Cs and Te thickness separately, the cathode on the left with anode grid to measure the photocurrent after preparation and evaporators on the right
We use the thickness monitors for rate control (0.01 Å/s)
halogen-light heating & Ar+ cleaning of cathodes
Diagnostic with 262 nm laser for QE & life time and QE distribution scan
Vacuum requirement: ~10-9 mbar

## Slide 11
Requirements for Transfer:
Load lock system with < 10-9 mbar to preserve QE ≥ 1 %
Exchange w/o warm-up & in short time and low particle generation
Cathode | Operation days | Q.E. in gun
#090508Mo | 30 | 0.05%
#070708Mo | 60 | 0.1%
#310309Mo | 109 | 1.1%
#040809Mo | 182 | 0.6%
#230709Mo | 56 | 0.03%
#250310Mo | 427 | 1.0%
#090611Mo | From 2011-7-26 | 1.2%
cathode #250310Mo
fresh QE 15.5%, in gun 1%
total beam time 1013 h
extracted charge 35 C
STATUS – Cs2Te photo cathodes
Notes: After preparation the cathodes needs to be stored and later moved into the gun, this is done by a transfer system with the requirements shown above.
What we see at every cathode is an early q-drop right after preparation were we do not know were it comes from
But this is stabilized at about 1% which is enough and can be preserved in the gun
The table shows the operation days and the QE in the gun of the cathode being used in the gun
The best one was in operation for more than 400 days, with an QE of at least 1%
The total beam time was 1013h and the total extracted charge was 35C
Unfortunately the cathode died during a vacuum problem

## Slide 12
STATUS – Multipacting at cathodes
MP was expected in the gap between cathode and cavity at surface fields of 0.1-0.2 kV/m since the early design stage!
So biasing of the cathode up to -7 kV was considered in the cathode design (el. isolated)
multipact simulation
MP at 2 MV/m
During increase of RF field, a hard MP barrier was observed, depending on the bias voltage level, the position and the used cathode
MP characterized by high current (1 mA) measured at the high voltage power supply
Electron flash at view screens
(#040809Mo)
The onset level is different for every cathode and its positions!
Notes: Another Problem we have to deal with is multipacting!
MP was expected in the gap between cathode and cavity at surface fields of 0.1-0.2 kV/m since the early design stage!
So biasing of the cathode up to -7 kV was considered in the cathode design (el. isolated)
What we now see During increase of RF field, a hard MP barriers are observed, depending on the bias voltage level, the position and the cathode
MP characterized by high current (1 mA) measured at the high voltage power supply, Electron flash at view screens and it is not possible to get above this level not even in pulsed mode!

## Slide 13
Rounding all edges to reduce field enhancement factor
Anti multipacting grooves to suppress resonant conditions
Recently, a comparative study with a number of cathodes showed that cathodes with Cs2Te layer have more or less
strong multipacting:
-> increased secondary electron yield due to Cs pollution
Present activities:
Additional shielding of cathode stem in cathode
preparation system
Coating with TiN to reduce secondary electron yield
(A. Brinckmann, DESY)
STATUS – Multipacting at cathodes
Notes: Beside the biasing we also tried so round all edges at the cathodes to reduce the field enhancement factor, with minor success
More successful was the test with anti multipacting grooves to suppress resonant conditions
The diagrams show the measured cathode current during the field increase, after some processing during the first one the MP was completely gone at the second test
We plan to use Coating with TiN to reduce secondary electron yield

## Slide 14
STATUS - Injection in ELBE & longitudinal phase space measurement
Method of measurement: phase scan technique using the second ELBE cavity
C2 phase variation
energy spectrum
longitudinal beam ellipse
cavity transport matrix
from parabola fit

## Slide 15
Browne Buechner spectrometer pictures
Same energy spread measured as in the 180° magnet of the diagnostic beamline
Bunch compression in SRF-gun as expected from ASTRA simulation
Successful test of long. phase space measurement for future gun optimization
Ekin = 3 MeV (CW) and 10 pC
@ exit of C1
STATUS - Injection in ELBE & longitudinal phase space measurement
Notes: Preliminary results
pictures show the bunch for different phases
Same energy spread measured as using 180° bending magnet of diagnostic beamline
Bunch compression in SRF-gun as expected from ASTRA simulation
So far phase space measured at the exit of cavity 1 but projection to gun in progress
Successful test of long. phase space measurement for future gun optimization

## Slide 16
Fixed energy imprint for correlation betw. energy spread and long. bunch distribution
Spectrometer  longitudinal distribution transferred to transverse distribution
Combination with quadrupole scan
Tool for future emittance compensation
x
y
3 MeV, 10 pC
J. Rudolph, et al., Dipac2011
Ergebnisse stimmen ganz gut überein, tool um später die gunparameter mit emittanzkompensation zu optimieren
STATUS - Injection in ELBE & slice emittance measurement
J. Rudolph, T. Kamps, HZB
Notes: Another important tool for optimization is the slice emittance measurement
This is done in a similar way
Now we use a fixed energy imprint to get a correlation between energy spread and the longitudinal bunch distribution
In the Spectrometer  longitudinal distribution transferred to transverse distribution  longitudinal slices accessible
Combination with quadrupole scan technique allows then to reconstruct the vertical emittance for each slice

## Slide 17
Laser beam
from DRACO laser
Electron beam
from ELBE
Quadrupole triplet
Al beamdump
dipole magnet
x-rays
Pb shielding
Cam
Off-axis
parabola
(F/#=30)
ELBE – Thomson Backscattering (Laser Group)
Production of x-ray photons (some tens keV) in small-scale linear accelerators like ELBE
Head-on collision of ≤150 TW laser pulse and 20 - 30 MeV electron bunch of ELBE linac
Electrons are driven by the electric ﬁeld of the laser pulse to an oscillatory motion (undulator)
emit Doppler up-shifted radiation at an angular frequency of ωsc=(10-20 keV)/h (for ELBE)
A.D. Debus et al., Appl Phys B (2010) 100: 61–76
vacuum chamber
Notes: At the end of my talk i will present the results of our first user experiment driven by the srf-gun – the thomson backscattering
The idea of thomson is the x-ray production with some tens of keV in small scale acc like ELBE
Therefore one uses the head on collision of TW laser pulse and 20-30MeV bunches from ELBE
If both hits each other, Electrons are driven by the electric ﬁeld of the laser pulse to an oscillatory motion
And emit Doppler up-shifted radiation
17

## Slide 18
ELBE – Thomson Backscattering (Laser Group)
1st setup ELBE linac with therm. injector than switch to SRF-Gun (Eacc=6 MV/m, exit energy 2.85 MeV)
Switch to 10 Hz single bunch mode (10 pC, 24 MeV) and optimized temporal overlap with laser
CdTe detector found same X-ray spectrum but lower photon yield than with therm. gun
→ 1st Demonstration of the Reliability of the SRF-Gun during an user experiment with critical needs in terms of bunch phase stability and laser-bunch synchronization
Notes: In order to get a good starting point 1st setup ELBE linac with therm. injector than switch to SRF-Gun (Eacc=6 MV/m, exit energy 2.85 MeV)
Switch to 10 Hz single bunch mode (10 pC, 24 MeV) and optimized temporal overlap with laser
CdTe detector found same X-ray spectrum but lower photon yield than with therm. gun
We are very happy about this result because it’s a demonstration of the reliable gun operation during an experiment with critical needs in terms of bunch phase stability and laser-bunch synchronization

## Slide 19
DRACO laser
150 -> 500 TW
Penelope
1.5 PW laser
ion wake field acceleration
CBS x-rays
electron wake field acceleration
FUTURE - Center for High Power Radiation Sources
extension of ELBE building finished

## Slide 20
FUTURE - New cavities with high gradient
standard
RRR 300
Nb cavity
large grain
Nb cavity
Fabrication of two new cavities to approach the design value
of the acceleration gradient
collaboration with Jlab (fabrication, treatment and tests)
slightly modified design:
lower Lorentz force detuning
lower microphonics
better cleaning and simpler clean room assembly
half-cell stiffening
larger boring
modified choke-cell pick-up

## Slide 21
43 MV/m peak field
in vertical test @ JLab
after He tank welding
JLAB_FG_Cavity
FUTURE - New cavities with high gradient
many thanks to Peter Kneisel
and his co-oworkers at JLab

## Slide 22
FUTURE - New cryomodule with intregrated SC solenoid
„Old“ cold mass of the operating SRF gun
Design for the new cryomodule with
SC solenoid (2 K)
Niowave Inc. (NPS, HZB)
remote controlled xy-table for
alignment (77 K)

## Slide 23
FUTURE - UV laser system for 13 MHz and 500 kHz
Under development at Max-Born-Institut Berlin
Will support both operation modes:
13 MHz, 2…4 ps (FWHM) pulse length for 77 pC
500 kHz (250, 125 …), 10…15 ps (FWHM) pulse length for 1 nC
Courtesy I. Will, MBI

## Slide 24
SUMMARY
STATUS
Long lifetime of NC Cs2Te photo cathodes in SRF gun (>1 yr, total charge 35 C @ QE = 1%)
No Q degradation since 4 years (RF operation ≈ 2500 h, beam time ≈ 1400 h)
Strong MP at cathodes defeated by DC bias and grooves, further improvement needed
First successful use of SRF injector at the ELBE accelerator
- Slice emittance measurements (J. Rudolph and HZB)
- Longitudinal phase space
- Inverse Compton backscattering (together with DRACO Laser Group at HZDR)
But gun performance limited by low RF-field (Epk  18MV/m and Q0 3x109)
FUTURE
On new upgrade cavity built at JLab (Peter Kneisel) with Epk = 43 MV/m (8 MeV) is ready
Clean-room assembly of cold mass at JLab and final installation in new cryomodule with SC solenoid
13 MHz / 500 kHz UV-laser upgrade will allow high-average current operation (1mA)

## Slide 25
Acknowledgement
We acknowledge the support of the European Community-Research Infrastructure Activity under the FP7 programme since 2009 (EuCARD, contract number 227579) as well as the support of the German Federal Ministry of Education and Research grant 05 ES4BR1/8.
THANK YOU FOR ATTENTION