## Slide 1: Permanent Magnet Demagnetization Induced by high energy electron radiation*
Temnykh
CLASSE & CHESS Laboratory, Cornell University, Ithaca, NY, 14853, USA
*This work was supported by NSF awards DMR-0936384 and DMR-0807731

## Slide 2
Presentation outline
Scope of experimental data and observations.
  PM undulator radiation damage at APS
  PM demagnetization study at SPing8
  Experimental study at Cornell
Analysis and Discussion
Conclusion

## Slide 3
PM undulator radiation damage at APS, ref [1]
Found that PM blocks were demagnetized in regions close to the beam axis. This indicates that the damage is due to electromagnetic showers coupled with photo-hadron production, but not due to neutrons. (Two competing theories)
[1] S. Sasaki, et al., Radiation damage to advanced photon source undulators, In Proceedings of 2005 PAC, Knoxville, TN, p. 4126.
Beam direction
Magnetic field degradation in U25 undulator during 4 month run (May-August 2004)
There is no data on accumulated dose
~2.4%

## Slide 4
Study at SPing8/Pohang Accelarator laboratory
Direct irradiation by 2GeV electron beam, ref [2]
[2] T. Bizen et al. / Demagnetization of undulator magnets irradiated by high energy electrons, Nuclear Instruments and Methods in Physics Research A 467–468 (2001) 185–189
Permanent magnet blocks were irradiated by 2.0GeV electron beam from the linac of Pohang Accelarator laboratory.
Various arrangements and materials
Factor 10 (!) for plate with parallel and perpendicular magnetization but not big difference for cube.

## Slide 5
Study at SPing8/Pohang Accelarator laboratory
Heat treatment effect, ref [3]
[3] T. Bizen et al. / Baking effect for NdFeB magnets against demagnetization
induced by high-energy electrons, Nuclear Instruments and Methods in Physics Research A 515 (2003) 850–852
Permanent magnet blocks were first baked at 142degC, then irradiated by 2.0GeV electron beam from the linac of Pohang Accelarator laboratory.
“ … This thermal treatment will be a good stabilizing method for magnets used in a high-irradiation environment.”
PM material: NdFeBr NEOMAX 35EH,
Hcj = 1989 kA/m

## Slide 6
[4] T. Bizen et al. /Radiation Damage in Magnets for Undulators at Low Temperature, In Proceedings of EPAC 2004, Lucerne, Switzerland
PM Material NdFeB NEOMAX 50BH
At 300oK, Hcj = 1116 kA/m
143oK, Hcj = 3060 kA/m
PM blocks were irradiated by 2.0GeV electron beam at room and low temperatures
At room temperature (300degK) PM material will be demagnetized by 1.4 T reverse field. At low (143degK) temperature, demagnetizing reverse field is 3.8T (x 2.7 higher!).
Study at SPing8/Pohang Accelarator laboratory
Low temperature effect, ref [4]

## Slide 7
PM demagnetization study at Cornell
[4] A. Temnykh, Measurement of NdFeB permanent magnets demagnetization induced
by high energy electron radiation, Nuclear Instruments and Methods in Physics Research A 587 (2008) 13–19
East Transfer Line
PM assembly, on the right, was attached to the East transfer line beam pipe. Irradiation process was controlled by steering of electron beam on/off the assembly by bending magnet “B3”.
Copper spacers
PM blocks
Transfer line
Beam pipe
Setup

## Slide 8
PM demagnetization study at Cornell
Irradiation process
Single irradiation cycle assembly temperature record
(1) Electron beam tuned ON
(2) Electron beam OFF
Q – energy / radiation dose absorbed by material
C – material heat capacity (0.41J/g/degC)
D = 0.324Mrad
11 irradiation cycles, total absorbed dose ~3.2 Mrad

## Slide 9
PM demagnetization study at Cornell
V - block
H - block
The tested samples properties

## Slide 10
Magnetic moment change as a function of accumulated dose
Comparison with ref [2] data:
Material N35EH;
50x1013 electrons => ~3Mrad dose

## Slide 11
PM demagnetization study at Cornell
Reverse field distribution for V and H blocks
Reverse field
~5kOe
Reverse field
~0
V-block
Reverse field ~11kOe
H-block
PM grade, block type | Hci(kOe) | Reverse Field(kOe) | Demag. Temp. (0C)
N40, H | ~12 | 11 | 61.66
N40, V | ~12 | 6.1 | 114.6
N40SH, H | ~20 | 8.62 | 128.8
N40SH, V | ~20 | 6.68 | 149.5

## Slide 12
Correlation between demagnetizing radiation dose and demagnetizing temperature
Device, more resistive to temperature demagnetization, will be more resistive to radiation.

## Slide 13
Damaging doses estimation for LCLS undulator magnets.
For material N40SH (?)
Tdmg = 110degC, D1% ~ 1Mrad
Reverse field
maximum
~ 1075mT
Single PM block
Reverse field maximum 1105 mT
Tdmg = 110degC, D1% ~ 1Mrad
Half period
Reverse field [mT]
Reverse field [mT]

## Slide 14
Conclusion
Recipe to maximize radiation resistivity
    Use material with high Hcj
    Minimize reverse field in design
    Heat treat blocks before assembly
    Lower operating temperature
Correlation between demagnetization temperature and radiation dose can be used to predict/estimate the damaging radiation dose at design stage. Accuracy?
Thank you