## Slide 1: CBMM Ingot Nb cavities
G. Ciovati, P. Dhakal, P. Kneisel, G. Myneni
Jefferson Lab
Ingot Nb Workshop, Jefferson Lab, Dec. 4th, 2015

## Slide 2: Ingots from CBMM
Five 13” diameter ingots, labelled A-E received between 2004-2006
  RRR ~ 260, Ta content ~800 wt.ppm (~1500 wt.ppm for ingot C)
Seven 13” diameter ingot, labelled A-D, F-H in 2008
  RRR between 70-150, Ta content between ~600-1400 wt.ppm
SRF cavities were built at JLab from the following ingots:

## Slide 3: CBMM Ingot Nb SRF cavities
26 single-cell and 11 multi-cell cavities were built at JLab from 2004 from CBMM Ingots
All but 3 cavities were in the 1.3-1.5 GHz frequency range

## Slide 4: CBMM Ingot Nb SRF cavities

## Slide 5: Statistics on cavity performance
Considered cavities made of RRR≥100
Most of the cavities have been tested multiple times, after different treatments (not the same for all cavities).
Compiled a statistic of the highest field achieved for each cavity, and the Q0-value at 2 K at the maximum field

## Slide 6: Quench field statistic
Only ~5% of the cavities were treated by EP
RRR~260: <Bp,max> = (119 ± 4) mT
RRR~100-150: <Bp,max> = (104 ± 8) mT
Electropolished
For a ILC/XFEL cavity shape:
RRR~260: Eacc = 28 MV/m
RRR~100-150: Eacc = 24 MV/m

## Slide 7: Q0 statistics
LCLS-II
CEBAF Upgrade
XFEL
ILC
RRR~260: <Q0> = (1.1 ± 0.1)×1010
RRR~100-150: <Q0> = (1.8 ± 0.2)×1010

## Slide 8: Doping with Ti or N
“Doping” with N or Ti showed the capability of producing a Nb surface for which Q0 increase with increasing Bp. The quench field however is reduced significantly
Similar behavior was found with doping medium-purity ingot Nb cavities.
Nitrogen doping
Titanium doping

## Slide 9: Lower Rs for medium-purity Nb
~20% lower RBCS for RRR ~ 100-150 than for RRR > 300
Rres ~ 2-3 nW routinely obtained with medium-purity ingot Nb
“Flat” Q0(Eacc) after standard treatments (EP, BCP)

## Slide 10: Best case
Treatments:
100 mm CBP + 50 mm BCP + 800°C/2h + 20 mm BCP (solid symbols)
120°C/12h bake (empty symbols)
To be published
1.5 GHz Single-cell “F3F4”, ingot Nb of RRR~120
The equivalent Q0(2 K) at 1.3 GHz is ~3.8×1010 with no doping!

## Slide 11: Mechanical properties
For the same annealing temperature:
Medium-purity ingot Nb cavities: higher yield strength than high-purity fine-grain ones
High-purity ingot Nb cavities: lower yield strength than high-purity, fine-grain ones
Cavities annealed at 800°C/2h
G. Ciovati et al., Mat. Sci Eng. A 642 (2015) 117
Single-cell
9-cell with He tank

## Slide 12: Conclusions
On average, the performance of cavities made from CBMM ingots is acceptable for many SRF accelerator projects
For the same treatment, higher quench-field can be achieved with high-RRR cavities, compared to medium-RRR
The quench field depends mainly on processing method (EP better than BCP) rather than RRR-value
Higher Q0-value can be achieved with medium-RRR, instead of high-RRR