## Slide 1: Ingot-Nb Based SRF Technology for the International Linear Collider
Akira Yamamoto, M. Yamanaka (KEK),
and
G. Myneni (Jlab)
to be presented at “Ingot Nobium CARADA Workshop”,
JLab, 4 Dec., 2015

## Slide 2
d
n
Atom：
４E5 yrs
Proton,
1E-4 sec
Star
10E8 yrs
Nucleus
3 min.
Elementary
Particles
Study of Universe/Cosmos
History of the Universe
~ 300 k Years
Limit of optical astronomical observation
Earlier Period
- Elementary particle physics taking
a major role,
Very early universe
~ 10-10 ~ -34 sec,
Particle accelerators play major
role.

## Slide 3: Applied Superconductivy Particle Acceleratoes
Becoming inevitable fundamental technology
SC magnet technology
Electron Acc.
SRF technology
LHC
Proton Acc.
ILC

## Slide 4: A full set of Fundamental Particles
Higgs
Boson?
Force Carriers
Z
Z boson
W
W boson
g
photon
g
gluon
Generations of matter
n
t
t-neutrino
t
tau
b
bottom
t
top
III
n
m
m-neutrino
m
muon
s
strange
c
charm
II
ne
e-neutrino
e
electron
d
down
up
u
I
Leptons
Quarks
The Standard Model
© Brian Foster
Particles and
Forces
Discovered at LHC
Nobel prize in 2013
Water
Atom
Nucleus
Proton
Quark

## Slide 5: Important Energies in ILC
Discovery of a 125 GeV Higgs has reinforced importance of ILC
E cm (GeV)
200
300
400
500
600
Integrated Luminosity (ab-1)
1
2
HZ
tt
HHZ
ttH
nnH
New Physics beyond SM:
Direct or indirect DM searches
Evidence for BSM physics
Hints of a new mass scale
Physics confident:
 Higgs and Top Quark
Learn “everything” about H (125)
Probe dynamics of EWSB
K. Kawagoe
(modified)

## Slide 6: Linear Collider as a next Step for Electron-Positron Collider
e-e+ accelerator
Ring collider
-->> Linear Collider

## Slide 7: ILC Technical Design Phase
ILC-GDE
2005
2006
2007
2008
2012
2009
2010
2011
2013
Tech. Design：TDP1
Higgs
discovered
126 GeV
Selection of SC Technology
TDP 2
Ref. Design (RDR)
LCC
LHC
2004
TDR
1980’ ~ Basic Study
2013.6.12
2012.12.15
TDR completion
2014

## Slide 8: ILC Layout Proposed
Damping Rings
e- source
E+ source
e- Main Linac
e+ Main Linac
Parameters | Value
C.M. Energy | 500 GeV
Peak luminosity | 1.8 x1034 cm-2s-1
Beam Rep. rate | 5 Hz
Pulse duration | 0.73 ms
Average current | 5.8 mA (in pulse)
E gradient in SCRF acc. cavity | 31.5 MV/m +/-20% Q0 = 1E10

## Slide 9
9
ILC Accelerator: Functional View
Linear Acceleration by using
SCRF Cavity Technology
e-/e+ Sources
Ultra low-emittance beam
(ultimately parallel)
Final focusing and
Collision
SCRF Main Linac
Notes: 9

## Slide 10: SCRF Industrialization required
Parameters | Value
C.M. Energy | 500 GeV
Peak luminosity | 1.5 x1034 cm-2s-1
Beam Rep. rate | 5 Hz
Pulse duration | 0.73 ms
Average current | 5.8 mA (in pulse)
Av. field gradient | 31.5 MV/m +/-20% Q0 = 1E10
# 9-cell cavity | 16024 (x 1.1)
# cryomodule | 1,855
# Klystron | ~400

## Slide 11: ILC Accelerator Parameters

## Slide 12: SCRF Procurement/Manufacturing Model
Regional hub-laboratories responsible to regional procurements to be open for any world-wide industry participation
Regional Hub-Lab:
E, & …
Regional Hub-Lab:
A
Regional Hub-Lab:
B
Regional Hub-Lab:
D
World-wide
Industry responsible to
‘Build-to-Print’ manufacturing
ILC Host-Lab
Regional Hub-Lab:
C: responsible to
Hosting System Test and Gradient Performance
Technical Coordination
for Lab-Consortium
: Technical
coordination link
: Procurement link

## Slide 13
SRF Facilities anticipated for Hub/Consortium
AMTF @DESY/E-XFEL, CEA,
STF-CFF @ KEK
ASTA @ FNAL, TEDF @ JLab
FNAL/ASTA, ANL
Cornell
JLAB
KEK
DESY, INFN, E-XFEL
SLAC, LCLS-II
CEA-Saclay, LAL-Orsay
IHEP, PKU
IUAC, RRCAT

## Slide 14: Cavity/Cryomodule Fabrication
Purchasing Material/Sub-component
Manufacturing Cavity：
Processing Surface
Assembling LHe-Tank ：
Qualifying Cavity, 100 %：
Cryomodule Assembly:: CM 組立
Cavity String Assembly：
Qualifying CMs, 33 + 5 %：

## Slide 15
ILC is inevitable
next machine!
Courtesy: R. Geng

## Slide 16
FG Single + EP
LG single + BCP
FG End-single + EP
FG 9-cell + EP
LG 9-cell + BCP
F. Furuta et al., International Symp. On Supercond. Sci. & Tech. of Ingot Niobium, Sept. 22-24, 2010.
ILC baseline (2.0K)
G2 1.8K
PJ1-2 1.8K
1 TeV ILC
Goal set in TDR
Bright future
Courtesy: R. Geng

## Slide 17: Optimization for Mass-production in the ILC Preparation Stage
Seeking for the best cost-effective production technology for Nb disk/sheet
  Very clean surface
    Important for gradient stability
  Optimum (could be lower) residual resistance ratio
    to be optimized with RRR of ~ 150 +/- 50
  Optimum (medium) grain size
  Hoping, to slice with better mechanically stability.
    optimum solution anticipated

## Slide 18: Technical Specification for Nb Sheet
Electrical Properties
  RRR: > 300 (to be furher optimized)
Chemical contents
  see table
Microstructure
  Re-crystalized 100 %
  Grain-size: ASTM 6 or finer (to be further optimized)
  Local grain size: ASTM 4-5
Mechanical Properties
  Ultimate strength: > 140 N/mm2, RT
  Yield strength: TBD (> xx N/mm2, RT)
  Elogation; > 30 %
  Hardness: ≤ 60
Shape/size: TBD
  Rect. Sheet : ~ 300 mm sq. or
  Circular sheet: ~280 mm dia. with a center-hole
    Possibility of Blanking (in consortium: to be discussed)
  Thickness : 2.8 mm +/- 0.1 mm
  Flatness: 2 % or better
  Surface roughness: < 15 mm (RF side)
Chemical contents: Example

## Slide 19: FG-Nb rolled or LG-Nb sliced from Ingot
Foreign materials could be rolled in
Cleaness to be highy
secured
Courtesy: G. Myneni

## Slide 20: A Direction to be Investigated for the Nb disk Mass-production
Clean surface from the beginning of Nb sheets
  Direct slicing from Nb Ingot (having high purity)
    Proposed and patentend in the US, by G. Myneni, P. Kneisel (Jlab) and T. Carneiro (CBMM)
    (Patented in Japan and in Europe, by KEK, Tokyo-Denkai, and others)
  Keep clean surface w/ directly sliced Nb-sheets
    w/o additional rolling causing contamination and defects
On the other hand,
  necessary mechanical uniformity and stability for press-work with tighter tolerance in assembly.

## Slide 21: A Direction to be Investigated for the Nb disk Mass-production
Clean surface from the beginning of Nb sheets
  Direct slicing from Nb Ingot (having high purity)
    Proposed and patentend in the US, by G. Myneni, P. Kneisel (Jlab) and T. Carneiro (CBMM)
    (Patented in Japan and in Europe, by KEK, Tokyo-Denkai, and others)
  Keep clean surface w/ directly sliced Nb-sheets
    w/o additional rolling causing contamination and defects
On the other hand,
  necessary mechanical uniformity and stability for press-work with tighter tolerance in assembly.

## Slide 22: Nb Sheet directly cut out anticipated with medium grain size
RRR: ~ 200
Grain size : < ~ 1 cm
  To be optimized for press-work,
Size: > 260 mm
Thickness: ~ 2.8 mm
Cleanness:
  Min. surface work
  No rolling

## Slide 23
Efforts for Self Learning at KEK
EBW
Press
Trim
AMADA digital-survo-press SDE1522
150t, 50stroke/min, 225mmstroke
MORI VKL-253
Vertical CNC lathe
Chemical
process
SST EBOCAM KS-110 – G150KM
Chamber (St. St. chamber)

## Slide 24: Fabrication and evaluation of low-RRR, LG single cell cavity
Mechanical Engineering Center, KEK
Masashi YAMANAKA
Presented at TTC Meeting @SLAC, 2 December, 2015

## Slide 25: Objectives
H | C | O | N | Fe | Si | Ta | RRR
< 10 | < 30 | < 30 | 10 | 3 | 20 | 1034 | 100
Chemical compositions (unit: ppm) and RRR
Motivation
Reduce the niobium material cost
Approach
Use low RRR cheap niobium
Use sliced ingot sheet
Objectives
Manufacture a single cell cavity
Evaluate the performance
50 mm
Sliced ingot niobium（φ260）
Boundary was traced by felt pen
Ingot Nb kindly contributed by CBMM
1.3 GHz single cell cavity
fabricated by KEK-CFF
TESLA-like (end cell)
Courtesy: M. Yamanaka

## Slide 26: Fabrication
Press forming for cells（Same way to ordinary process）
Crack occurred
Just at surface, no leak
EB welding for equator part
EBW test (plate)
Welding bead across the boundary is smooth (not affected)
Deformation is not uniform due to anisotropy
It is difficult to keep circularity at edge (equator)
Leak check was achieved before trimming edge
Courtesy: M. Yamanaka

## Slide 27: Single-Cell cavity Fabricated
LG takes time to fabricate a cavity comparing with FG
Crack
Sputter
Bead is not uniform
Courtesy: M. Yamanaka

## Slide 28: Comparisons with high RRR Nb
Fine grain (TD)
Large grain (TD)
42
36
31
 | H | C | O | N | Fe | Si | Ta | RRR
LG (TD) | < 5 | < 10 | < 10 | < 10 | < 10 | < 10 | 80 | 390*
FG (TD) | < 10 | 40 | 100 | 40 | 20 | 20 | 700 | 258**
LG (CBMM) | < 10 | < 30 | < 30 | 10 | 3 | 20 | 1034 | 100*
Measurement RRR: * by KEK, ** by TD
The effect of low RRR and high Ta not seen on Q0.

## Slide 29: Progress and Comments
A single cell cavity using low RRR large grain niobium was fabricated and evaluated.
The maxim gradient reached 31 MV/m.
Multiple repairing/inspection and tests required to reach the high gradient. LG requires moretime in fabrication, compared with FG. . It causes higher cost.
Smaller grain size would be an important issue for mass production.
φ260×500 niobium ingot was provided by CBMM

## Slide 30: Key Issues to be Settled
Fabrication of Nb sheets
  Size: 260 mm diameter, ~ 3 mm thick
  Quantity: ~ 18,000 x 20 = 360,000 disks (~1.2 kg/disk)
  Purity, Residual Resistance Ratio
    RRR: 150 ~ 200 to be investigated (currently > 300 )
  Mechanical uniformity
    Grain-size : to be optimized (with a level of thickness?)
    How it can be made with cost-effective process?
      Adding specific, controlled impurities, contolling environment?
Best cost effective solution anticipated
  Nb Ingot with medium grain-size to be optimized

## Slide 31: Acknowledgments
I would thank CBMM (specially for Mr. R. Ribas, and Mr. G. Abdo) for their kindest cooperation for the R&D effort to seek for the most optimum properties for the ILC and furher applications.
I would thank Dr. G Myneni for his kindest guidance to realize the optimum Ingot-Nb material for future, various SRF applications.