## Slide 1: Muon2011
HCC:
Helical Solenoid Development
HTS Coil Progress
J. Tompkins
Fermilab – TD/MSD

## Slide 2: Acknowledgements
The ongoing design, fabrication, and test effort for Muon Collider magnets has a large list of contributors – acknowledgements for this presentation include:
  Fermilab:
  Emanuela Barzi Vadim Kashikhin Vladimir Kashikhin
  Mike Lamm Vito Lombardo Mauricio Lopes
  Sasha Makarov Mike Tartaglia Katsuya Yonehara
  Miao Yu Sasha Zlobin
  Muons, Inc.
  Gene Flanagan Rolland Johnson Steve Kahn

## Slide 3: Outline
Overview
Helical Solenoid Development – HCC
HTS – YBCO Coil Development
Summary

## Slide 4: Helical Cooling Channel
The helical solenoid (HS) concept (FNAL/Muons Inc.) :
    Coils follow the helical beam orbit generating solenoidal, helical dipole and helical quadrupole fields
    Multi-section HCC
  Would require 160 meters of magnets
  Wide range of fields, helical periods, apertures
  Room for RF system
  Field tuning is more complicated at high fields
  NbTi, Nb3Sn/Nb3Al and HTS in final stage
Early Specs, ca. 2006-K. Yonehara, S. Kahn, R. Johnson et al.

## Slide 5: HS Mechanical Concept (FNAL)
Hoop Lorentz forces intercepted by stainless steel rings around the coils
Transverse Lorentz forces intercepted by support flanges
Outer LHe vessel shell provides mechanical rigidity to the structure
The peak stress is ~60 MPa
HSM01

## Slide 6: 4-Coil NbTi Model Fabrication 2010-11

## Slide 7: HSM01 – First Helical Solenoid Model
The first helical solenoid model (HSM01) designed, fabricated and tested at Fermilab.
NbTi SSC cable was used for this model. Left picture shows the winding process.

## Slide 8: Helical Solenoid Development HSM01 – 1st Model
Solenoid Parameters |  | 
Parameter | Units | Value
Coil inner diameter | mm | 426
Coil outer diameter | mm | 455
NbTi SC cable cross section | mm | 12.34 x 1.46
Cable Ic (7T,4.2K) | A | 9660
Jc (non-Cu) | A/mm2 | 1730
Copper to superconductor ratio |  | 1.5:1
Strand diameter | mm | 0.8
Helical Orbit Radius | mm | 255
Number of turns/coil |  | 10
Coil width | mm | 20
HSM01 tested in Nov/Dec 2008 (TD-01-011, PAC09)
  Ground insulation issues
  Epoxy voids; packing factor
  SC lead support
  Coordinate system (measurements)

## Slide 9
A second model HSM02 was been built to improve the solenoid manufacturing technology and performance.
HSM02 baseline magnetic and mechanical design is the same as for HSM01
Improved:
  mechanical structure and insulation
  cable geometry and insulation
    Additional flattening
  coil winding and impregnation procedures
SSC cable re-sized (flattened):
    cable test => no degradation
HSM02 was tested at Fermilab MTF at the end of 2010

## Slide 10: HSM02 Ready for installation in VMTF
Top plate
30kA power leads
Instrumentation ‘tree’
HSM02
Start: 11/9/2010 |  |  | 
 |  | Quench | Quench Total
1 | Initial Check-out | - | -
2 | 4.0K Quench Testing, 20 A/sec nom. | 29 | 29
3 | 4.0K Ramp Rate Studies | 13 | 42
4 | 3.0K Quench Testing, 50A/sec | 13 | 55
5 | 4.0K Quench Testing, 20 A/sec nom. | 2 | 57
6 | 3.0k, 250 A/sec | 16 | 73
7 | 4.5K | 7 | 80
8 | 4.5K Heater Tests | 17 | 
End: 11/22/2010 |  |  | 

## Slide 11: HSM02 Quench Test Results

## Slide 12: Comparison of Quench Results with HSM01

## Slide 13: HSM01, HSM02 Comparison of Test Results

## Slide 14: HSM, the next steps
Further development of outer field coils (NbTi, Nb3Sn) – depending on resources available, priorities, etc.
  HSM03 – same design but with Al rings for coil pre-stress
  HSM04 – Nb3Sn design
      Needed for inserts in higher field cooling section
      Different technology – used in LARP/High Field Magnet Program
  Helical solenoid inner coils using HTS (BSSCO wire or YBCO tape) materials
    HTS required for inserts in higher field cooling regions
    Different technology
      Collaboration with Muons, Inc. to design, build, test first model
      YBCO coil development under way
    Final cooling section >40T fields (but smaller aperture)

## Slide 15: HCC - Hybrid HS Model
Conceptual design study shows that a Hybrid HS may be needed for HCC
The goal - develop mechanical design and technology for HTS section based on G2 tape/cable and its assembly with RF and Nb3Sn section
Support structure was designed and prototyped
12-mm YBCO tape procurement has been initiated by Muons Inc.
This work is partially funded by, and performed in collaboration with, Muons Inc. (SBIR funded)

## Slide 16: High Field Final Cooling Solenoid ‘Generic’ Design
5
Nb3Sn
NbTi
Basic Parameters
  Inner bore diameter 50 mm
  Length 1 meter
  Fields 30 T or higher  HTS materials
Key design issues:
Superconductor type
Jc, effect of field direction (in the case of HTS tapes)
Stress management
Quench protection
Cost
Conceptual design:
Hybrid coil design
Coil sections
B
Coil radius, m
YBCO / BSCCO
50T Solenoid Conceptual Design

## Slide 17: FSU-NHMFL/ASC Superconductors – Je plot
Peter Lee, FSU-NHMFL

## Slide 18: YBCO Tape (from SuperPower)

## Slide 19: Insert Coil R&D
Present focus on single and double-layer pancake coils based on HTS tapes.
~20 single and double-layer pancake coils (YBCO and Bi-2223) were built and tested in self-field and external solenoid
  Study tape splicing techniques, effect of coil impregnation, coil preload
A modular HTS Insert Test Facility to test up to 14 double-layer pancake coils inside the 14T/16T solenoid (B>20 T)
For the second phase of the coil program, larger multi-section HTS coils will be designed, fabricated and tested to achieve higher magnetic field and force levels.

## Slide 20: YBCO Coil Parameters
Conductor | SuperPower SCS4050-i
Turn to Turn Insulation | Spiral Wrapped Kapton
Coil Geometry | Double Pancake
Coil ID | 19 mm
Coil OD | 62 mm
Conductor Thickness | 0.1 mm
Conductor + Insulation Thickness | 0.2 mm
Turns per Single Coil | 108
Conductor length per Coil | 13.9 m
Overall Conductor Length | 27.8 m

## Slide 21: YBCO coil Current vs. Field
From: “Test of 1st YBCO Helical Solenoid Double Pancake Model”, M. Yu, et al., FNAL TD-11-001, 2/2011
Radial Component Distribution (Field ┴ to the Tape)

## Slide 22: Winding Development

## Slide 23: Magnetic Simulations

## Slide 24: YBCO coil in 13.5T Background Field
Chart: Current (A)
Chart: Current (A)
Voltage (V/cm) vs. Current (A)

## Slide 25: Looking ahead
Focus on high field (HTS) solenoids necessary for cooling sections
Conductor development has dominated the R&D path
  Quality (Jc, stability, uniformity)
  Length
YBCO based solenoid efforts are underway and will continue
  PBL/BNL (mostly SBIR funding)
  Fermilab/Muons Inc. (SBIR & FNAL/MAP funding)
  YBCO is being produced in industry on pilot lines that can yield 100-200 m lengths – the tapes are not optimized for magnets but various projects using the tapes are underway. R&D support would enhance progress for this very promising technology.

## Slide 26: Looking ahead, cont.
VHFSMC (an ARRA funded collaboration) is focused on Bi2212 development
  Phase I – improvement of strand properties
  Phase II – development of small solenoid coils (beginning now) for possible use in MC…
  Future – proposal to DOE being developed
A Fermilab Bi2212 solenoid development initiative will be discussed in the next talk by Tengming Shen

## Slide 27: Other Fermilab Magnet Efforts
LARP Collaboration – BNL, FNAL, LBNL
  2nd generation large aperture IR quadrupoles for LHC upgrade
CERN/Fermilab collaboration to develop 11T Nb3Sn dipoles to replace NbTi before IR collimators
  More space in lattice
Mu2e experiment
  3 large NbTi solenoids – initial designs, model tests, design, fab, procurement TBD
Ongoing development for ProjX & ILC
  SC solenoids, split quads, corrector dipoles

## Slide 28: Backup Slides Follow

## Slide 30: Winding Development, details

## Slide 31: Double Pancake Winding