## Slide 1: SRF photo-injectors
J. Sekutowicz
May 19th, 2014
Cool sources keeping us busy

## Slide 2
Outline
Introduction
  History and goals
  Applications
  Two approaches
R&D programs
    Cavities for SRF injector
    Cathodes
Final remarks

## Slide 3
  Introduction a. History and goals
Milestones in history of NC and SC photoinjectors
Date Milestones
1985 First photoinjector at Los Alamos , R. Sheffield et al.
First FEL driven by photoinjector at Stanford
1988 First proposal for SRF photoinjector by H. Piel
1991 First photocathode in a sc cavity at Wuppertal, A. Michalke
1993 UV FEL driven by photoinjector at Los Alamos
...............................
2013 First IR FEL driven by photoinjector J. Teichert, et al., HZDR
3 years
22 years
???? UV- or X-FEL driven by SRF photoinjector ?

## Slide 4
  Introduction a. History and goals
Result of the first photocathode in a sc cavity experiment was published in 1992 at EPAC by H. Piel and A. Michalke.
Eacc = 1.5 MV/m, Qo 1.5E7 and electron current of 0.5µA.
Important step but expectations nowadays are far from this result.

## Slide 5
  Introduction a. History and goals
SRF photoinjectors have unique potential to generate
high brightness electron beams at high duty factor
q/bunch
~ 1nC
low ɛn
+
≤ 1mm·mrad
high DF
+
-> 100%
SRF photoinjectors seem to be the best choice for this spec
Courtesy A. Arnold

## Slide 6
  Introduction b. Applications
Potential application of SRF injectors in accelerators
Facility | Ibeam [mA] | q [nC] | Ɛn [µm] | frep [MHz] | Ecath [MV/m]
ELBE at HZDR (operation at low q) | 0.5 | 1 | ≤ 1 | 0.5 | 30
E- XFEL upgraded to cw/lp mode | 0.2 | 1 | ≤ 1 | 0.2 | 50+
FLASH upgraded to cw/lp mode | 0.2 | 1 | ≤ 1 | 0.2 | 50+
ERL BERLinPro at HZB | 100 | 0.077 | ≤ 1 | 1300 | ≥ 10+
ERL at BNL | 500 | 0.7 | ≤ 1.4 | 704 | 30
WiERL | 1 | 0.2 | ≤ 0.9 | 5 | 45
Parameters of SRF injectors* for future applications
*I will not discuss DC-SRF hybrids (like Cornell or PKU designs).

## Slide 7
  Introduction c. Two approaches
Two approaches to SRF photo-injector design
sc-cavity & nc-cathode
Ibeam up to 500 mA
sc-cavity & sc-cathode
Ibeam ~ 1 mA
Cons: Load lock system makes integration of nc-cathode with sc-cavity very challenging.
Pros: QE of nc cathodes is high.
Pros: There is no load lock system. Integration of sc-cathode with sc-cavity is less challenging.
Cons: QE of metallic sc-cathode is low.

## Slide 8
  Introduction c. Two approaches
Two approaches to SRF photo-injector design, cont.
sc-cavity & nc-cathode
Ibeam up to 500 mA
sc-cavity & sc-cathode
Ibeam ~ 1 mA
HZDR
1.3GHz
HZB
1.3GHz
Univ. Wisconsin
200 MHz
JLab/DESY, 1.3GHz
before Febr. 2012
JLab/DESY, 1.3GHz
after Febr. 2012
Plug option

## Slide 9
  Introduction c. Two approaches
sc-cavity & sc-cathode = all superconducting photo-injector
The story began in 2002 with these two at BNL
Cathode was the back wall made of Nb
QE = 10-5 @ λ =260 nm and 48 MV/m
Plaser = 0.5W, spot 6 mm2, no quench!
Triveni Rao
John Smedley

## Slide 10
  Introduction c. Two approaches
The result showed that for 1nC & frep. of ~200 kHz, one will need UV laser with power of 93 W on the cathode. Quenching guaranteed!!!
In 2004 we began to look for a better sc-cathode:

## Slide 11
and the first choice was Pb cathode (Tc=7.2K)
Chart: 
| 6.5306524738813332 | 6.4291397411267006 | 6.2041198501872659 | 5.9086855716069193 | 5.8254646480631598 | 5.6401089547156973 | 5.3948868262497962 | 5.1700998751560547 | 5.0033224598284409 | 4.963295880149813 | 4.7723998847594347 | 4.6647517670580942 | 4.5956443334720483 | 4.4315141787051893 | 4.2787033449567353 | 4.1360799001248436 | 4.0682753115982067 | 4.0026579678627519 | 3.9391237144046132
Pb: arc-deposited | 0.0055274 | 0.0054224 | 0.0041305 | 0.0030281 | 0.0027287 | 0.0021292 | 0.0014079 | 0.00099367 | 0.00074278 | 0.00068756 | 0.00046281 | 0.00035595 | 0.00028995 | 0.00017421 | 9.9924e-05 | 4.6134e-05 | 3.1106e-05 | 1.9888e-05 | 1.3017e-05
190 nm
193 nm
200 nm
210 nm
213 nm
220 nm
230 nm
240 nm
Eɣ [eV]
QE
248 nm
  Introduction c. Two approaches
For this QE laser P will drop from 93 W to 2.6 W !!!
Courtesy T. Rao & J. Smedley

## Slide 12
  Introduction c. Two approaches
Smooth back wall option (JS)
Plug option (PK)
Back wall with stiffening slab,
no plug
Back wall with plug

## Slide 13
  Introduction c. Two approaches
After several tests we decided to proceed with no-plug option. We build a number of cavities, both 0.5 and 1.6-cell. All cavities were tested before the coating (baseline test).
Chart: Baseline test, 1.6-cell
| 1.6069325582363434 | 2.5007137482246944 | 3.6054115246945106 | 5.0084470472672455 | 6.3562782544504763 | 8.340394163922948 | 9.8649267564640333 | 11.447440542304641 | 13.107154242351768 | 14.818150086971047 | 16.754341766980879 | 18.837127072672203 | 21.534805131786076 | 23.560392654113382 | 25.836327503730086 | 28.610927779713819 | 30.397079184948016 | 32.626861158499445 | 35.907652426523235 | 37.440395559448888 | 39.937594857577487 | 41.406058520173097 | 44.592538524197067 | 45.835774335075868 | 47.195284620054998 | 48.552907358797782 | 48.805506872237281
"Baseline #1" | 12063890276.6446 | 12150291724.5881 | 12246386965.5342 | 12371767711.5809 | 12495390069.5158 | 12456833210.8744 | 12134942841.1544 | 11919518003.7181 | 11879012910.4672 | 11624323583.1562 | 11437124184.3723 | 11259617301.5815 | 10994302222.9356 | 10759936015.016 | 10620562355.3086 | 10460496477.8855 | 10422560471.1572 | 10264786029.7427 | 9888992474.9328 | 9274142239.8217 | 8761219510.8209 | 8174554169.1376 | 6434913943.337 | 5664723017.9589 | 4711958239.1322 | 3810042876.297 | 3648055311.1261
Courtesy P. Kneisel

## Slide 14
  Introduction c. Two approaches
Pb coating took place at NCBJ in Świerk:
Arc-deposition setup
Pb spot on the back wall
FPC port
Pickup port

## Slide 15
  Introduction c. Two approaches
The route to coat the back wall was long:
JLab->DESY->Świerk->DESY->JLab = 11000 miles
and it took a lot of time, especially when we wrote down in the shipment documents “gun cavity”.

## Slide 16
  Introduction c. Two approaches
Back at JLab: preparing for the vertical test we used mask to protect coating from the BCP acids. For HP rinsing (no jets directly on the Pb-spot) the mask had to be disassembled.
In most cases, after the preparation
Pb spot was partially damaged
…or totally removed
In February 2012, we decided to proceed with plug even though the first results for plug version were not very encouraging.

## Slide 17
Present design of the SRF-injector cavity with sc-cathode.
Cathode
1.6 cells
Plug
Plug
Pros:
Pb-coated plug is assembled after BCP and HP rinsing.
Preparation of the substrate and coating is technically simpler.
Shipment is easier.
Cons:
Cooling of the cathode requires more attention.
Plug, if improper installed, may cause leaks.
  Introduction c. Two approaches

## Slide 18
Present design of the SRF-injector cavity with sc-cathode, cont.
  Introduction c. Two approaches
Chart: Ecathode [MV/m]
| 11.358254552063638 | 6.2024618972504184 | 3.734571091831453 | 5.4440260960872733 | 7.6535932219945764 | 9.4907593044304406 | 8.488793185118034 | 10.780778125883421 | 13.291435928419478 | 14.703021091568873 | 16.420792022277769 | 18.672855459157265 | 20.737240773503302 | 23.071872716748221 | 25.51197740664859 | 28.257157783236909 | 30.682632444041758 | 31.835256296060667 | 30.701566498570703 | 34.091813826713071 | 34.599412178462252 | 35.917954628496645 | 38.115806596398826 | 41.19329537914011 | 41.474481547006604 | 44.450286939365753 | 47.115824100730258 | 49.521220044441634 | 51.590275762871769 | 52.814810877145376 | 53.903890629417099
Jlab Baseline Test with Nb-plug, 2012 | 19875432788.6236 | 20462161731.6261 | 19841619294.8444 | 20570549147.5428 | 20750198546.0321 | 20071110272.3892 | 20657179179.3206 | 20000794944.1552 | 20107927349.7158 | 19776224209.65 | 19543841322.137 | 19218332272.4379 | 18920305000.1186 | 18512472816.2062 | 17893676287.56 | 17591471921.6181 | 16450661174.0363 | 16007611442.8471 | 10231899883.8232 | 16034669555.7963 | 16076727183.6198 | 15547161828.5212 | 14310144125.2194 | 13326545148.4835 | 13555672587.5697 | 12383861487.9048 | 11506653167.3131 | 9853026925.2149 | 7662381963.4186 | 6323527871.7366 | 5225843972.4168
Jlab with Pb plug, 2012 | 1613479261.8878 | 2090419193.1985 | 2351616006.8812 | 2694387879.6433 | 3146139838.84 | 3886721282.5795 | 4678722649.9711 | 5847525841.2708 | 6905605125.0163 | 8811259857.5967 | 10447350090.4052 | 11811047284.5545 | 13268155903.9357 | 14303046944.2156 | 14889984005.7636 | 15334984072.193 | 15416196827.0505 | 15623679967.8878 | 15727350464.8578 | 15907625619.7259 | 16051883878.9376 | 15975335023.628 | 15714075690.0313
DESY baseline T1 with Nb-plug, 2013 | 16400000000 | 16200000000 | 16000000000 | 15700000000 | 15500000000 | 15200000000 | 14900000000 | 14600000000 | 14000000000 | 12900000000 | 12000000000 | 10500000000 | 8900000000 | 7220000000 | 5680000000 | 4400000000 | 3340000000 | 2440000000 | 1770000000 | 1260000000 | 913000000 | 658000000 | 477000000 | 351000000 | 306000000 | 310000000
DESY baseline T2 with Nb-plug, 2014 | 19900000000 | 19900000000 | 19600000000 | 19000000000 | 18300000000 | 17600000000 | 15800000000 | 13800000000 | 11600000000 | 9420000000 | 7500000000 | 5920000000 | 4500000000 | 3390000000 | 2490000000 | 1800000000 | 1290000000 | 917000000 | 659000000 | 474000000 | 346000000 | 292000000

## Slide 19
  Introduction c. Two approaches
We could not reassemble Jlab good results neither at HZB nor at DESY
Maximum Eacc was 24 MV/m only and Qo was low.
QE (test at HZB) was by factor of 4 lower than for Pb-samples.
Recent improvements.
Better cooling of the cathode plug with additional channels for LHe.
Helium channels
Sealing
surface
Cathode post

## Slide 20
  Introduction c. Two approaches
Recent improvements, cont.
Present Pb coating is better as compared to the coating on tested plug
Before Pb coating
Roughness < 0.5µm
After Pb coating
droplets ø < 20µm
and height of few µm
Plug tested at HZB was rough and coating showed many large droplets

## Slide 21
sc-cavity & nc-cathode
  Introduction c. Two approaches
HZDR 1.3GHz, 3.5-cell is the most advanced SRF source, driving ELBE
Chart: Ecathode [MV/m]
| 3.8016000000000001 | 4.0175999999999998 | 4.1256000000000004 | 2.6676000000000002 | 2.4407999999999999 | 2.052 | 1.5768 | 0.97199999999999998 | 3.1751999999999998 | 3.8555999999999999 | 4.2984 | 4.6656000000000004 | 5.2595999999999998 | 5.6592000000000002 | 6.3503999999999996 | 7.0956000000000001 | 6.7392000000000003 | 7.7220000000000004 | 7.4088000000000003 | 8.2943999999999996 | 7.9379999999999997 | 8.8884000000000007 | 8.5968 | 9.4391999999999996 | 9.1476000000000006 | 10.151999999999999 | 9.7956000000000003 | 11.9016 | 11.61 | 11.307600000000001 | 12.1608 | 12.9924 | 13.024800000000001 | 12.906000000000001 | 13.5756 | 13.608000000000001 | 13.456799999999999 | 14.245200000000001 | 14.104799999999999 | 13.3164 | 11.5128 | 14.3208 | 14.4072 | 14.5152 | 14.5692 | 14.7204 | 14.806800000000001 | 10.638 | 9.9144000000000005 | 8.8452000000000002 | 8.0676000000000005 | 7.1711999999999998 | 6.5232000000000001 | 5.1947999999999999 | 4.0284000000000004 | 3.3048000000000002 | 2.3435999999999999 | 1.4688000000000001
HZDR, Gun 2, 3.5-cell, 2011 | 19600000000 | 19400000000 | 19300000000 | 19700000000 | 19800000000 | 19500000000 | 19200000000 | 19100000000 | 19900000000 | 19700000000 | 19600000000 | 19500000000 | 19300000000 | 19500000000 | 19300000000 | 19200000000 | 19300000000 | 19100000000 | 19000000000 | 19200000000 | 18900000000 | 18900000000 | 18900000000 | 18700000000 | 18700000000 | 18400000000 | 18600000000 | 17100000000 | 17400000000 | 17700000000 | 16700000000 | 14900000000 | 15000000000 | 15300000000 | 13400000000 | 13500000000 | 14000000000 | 11800000000 | 12200000000 | 14500000000 | 17600000000 | 10300000000 | 10400000000 | 10500000000 | 10500000000 | 8800000000 | 8880000000 | 17800000000 | 18300000000 | 19000000000 | 19100000000 | 19300000000 | 19400000000 | 19700000000 | 19900000000 | 20100000000 | 20000000000 | 20000000000
HZDR, Gun 1, 3.5-cell, 2007 | 2985810000 | 2758420000 | 2776420000 | 2736220000 | 2655910000 | 2352480000 | 1798780000 | 1268420000 | 1005300000 | 838710000
Significant progress

## Slide 22
  Introduction c. Two approaches
HZDR lasing with Gun 1
Ekin at gun exit | 3.3 MeV
Micro pulse repetition rate | 13 MHz
Macro pulse repetition rate / length | 1.25 Hz / 2 ms
Beam energy at FEL | 27.9 MeV
Bunch charge / beam current | 20 pC / 260 µA
RMS bunch length | 1.6 ps
Normal. RMS emittance | 1 mm mrad
ELBE infrared FEL (20 – 250 µm)
April 11, 2013!
before
first lasing
optimized
Congratulations!!!!
Courtesy A. Arnold

## Slide 23
  Introduction c. Two approaches
Gun 2 is now being assembled and prepared for testing.
Courtesy A. Arnold
We are waiting for good news from Rossendorf.

## Slide 24
  Introduction c. Two approaches
HZB: 1.5-cell, 1.3GHz
Chart: Ecathode [MV/m]
Cavity is still at JLab for testing and further improvement of the performance ( mainly to remove the multipacting barriers).
Courtesy A. Neumann

## Slide 25
  2. R&D programs a. Cavities for SRF injector
Shape of the back wall for all sc injector (we follow studies of Rama Calaga at BNL):
α
1 m
Solenoid
B
Ecath
lcs
Chart: Slice number
0 deg | 2.3 | 1.53 | 1.46 | 1.55 | 1.41 | 1.59 | 1.43 | 1.41 | 1.41 | 2.27
5 deg | 2.06 | 1.25 | 1.16 | 1.24 | 1.06 | 1.24 | 1.12 | 1.13 | 1.18 | 2.15
8 deg | 1.71 | 1.14 | 1.07 | 1.15 | 0.932 | 1.14 | 0.998 | 1.12 | 1.08 | 2.05
10 deg | 1.6 | 1.13 | 1.07 | 1.09 | 0.947 | 1.13 | 1.01 | 1.14 | 1.05 | 1.95
12 deg | 1.5 | 1.12 | 1.04 | 1.07 | 0.914 | 1.1 | 1.05 | 1.12 | 1.05 | 1.89
Parameter | Unit | Value
Bunch charge, Q | nC | 1
τ | ps | 20
Ecath | MV/m | 60
B | T | 0.25
Cath.-to-solen. dist., lcs | m | 0.41
8° seems to be optimal.
Fixed parameters for investigation ɛx vs. α

## Slide 26
  2. R&D programs b. Cathodes
Alternative emitter to Pb could be cesiated p-GaN (support by BNL and NCBJ)
Pros: High QE at 4-th harmonic for thin coatings of ≥ 30 nm.
Cons: GaN after cesiation must be transported and assembled in an inert gas.
QE measured in April, 2014 at SVT company. Deposition on Nb, QE at 300K.
Chart: Wavelength [nm]

## Slide 27
GaN is not a superconductor but if coating is thinner than 40nm it should behave like a superconductor (proximity effect).
Next steps:
Coating of Nb-plug with 30 nm GaN (no Cs) and vertical test to prove proximity effect in the sc gun cavity
QE test at 70K of 30nm GaN on Nb.
The third choice is Nb3Sn multifilament (4µm) wires as emitters. We follow here PSI approach, in collaboration with BNL and NCBJ. Unlike PSI we want to take advantage of the fact that Nb3Sn is an excellent superconductor and use it in sc cavity. This R&D program is at very early stage.
A. Anghel et al.
Measured max. QE=1% @ 266nm
  2. R&D programs b. Cathodes

## Slide 28
  3. Final Remarks
1. Technical remark
LCLS showed in 2009 that SASE process takes place with 20 pC !
The nominal charge of LCLS II bunches will be ≤ 300 pC.
Assuming:
QE = 2·10-4@260nm
(half of QE measured for Pb)
q/bunch
+
300 pc
frept.
+
200 kHZ
the required laser power will be 1.4 W@260nm (7µJ/pulse).
Technical remark
The list of type 2 superconductors is rather long, more than 140
are listed. Is there really no good photo-emitter among them?

## Slide 29
Dear Peter,
the DESY SRF group thanks you for your contribution to our SRF programs and projects based on the SRF technology.
  3. Final Remarks
We built for you a “mini-gun”, just in case you will need one.
Thanks and enjoy the family life in Denver.

## Slide 30
Acknowledgements
I want to express my gratitude to all Colleagues contributing to the experiments and R&D program on sc-cathodes:
DESY: R. Bandelmann, D. Klinke, D. Kostin, A. Matheisen, W.-D. Möller, D. Reschke, M. Schmoekel, X. Singer, W. Singer, N. Steinhau-Kuehl
HZB: T. Kamps, O. Kugeler, A. Neuman
NCBJ: M. Barlach, J. Lorkiewicz, R. Nietubyc,
JLab: G. Ciovati, P. Kneisel
BNL: T. Rao, J. Smedley
HZDR: A. Arnold, J. Teichert
Thank you for your attention

## Slide 31
Parameter Calc Value Units
Temperature 4.2 K
Cavity Frequency 199.6 MHz
Unloaded Q (Q0), Nominal 3 x 109
Surface electric field, Pk /Ecath 53 /40 MV/m
Integrated Electric Field 3.96 MeV
Dynamic heat loss at EPK 39.2 Watts
Static Heat Loss at 4.2K 7.5 Watts
Test 2012, fall
Ecath = 5 MV/m
  Backup WiFEL Wisconsin

## Slide 32
At 25% duty factor, the Boeing gun delivered 32 mA, the highest average current for any electron injectors. The measured rms emittance was:
5-10 microns for bunch charge between 1 and 10 nC.
At duty factor between 1% and 25%,
the average photocathode lifetime was 2.3 hours.
  Backup Boeing (status 2008)
The Boeing 433-MHz re-entrant RF injector cavity design.