## Slide 1: PURIFICATION OF 6 GHZ RESONATORS AT EXTREMELY HIGH TEMPERATURES AT ATMOSPHERIC PRESSURE
A.A. Rossi, S. Stark, R. K. Thakur, N. Visonà and V. Palmieri
ISTITUTO NAZIONALE DI FISICA NUCLEARE
Legnaro National Laboratories
and University of Padua
5th Workshop on Thin films and New Ideas for pushing the limit of SRF,
July 18--20, 2012, Jlab, Newport News VA

## Slide 2: There is a plenty of incredible games to play just close to the melting point of Niobium ….

## Slide 3
6 Ghz @4,2K
Bulk Nb
BCSNB

## Slide 4
Nb5N6; Nb4N3
d-NbN 1-x; h-NbN (hexagonal);
d’-NbN (hexagonal);
b-Nb2N (hexagonal); g-Nb4N3-x
a-Nb (N) (bcc solid solution)
Niobium

## Slide 5
1 – 3 mm of nitridation in a couple of minutes

## Slide 6
SC 1
SC 2
a
l1
l2
Vacuum
Hz
Niobium
Overlayer

## Slide 7
SC 1
SC 2
a
l1
l2
Vacuum
Hz
For a “2 Superconductor system”
l1/a
Q2
Q1
DQ

## Slide 8
SC 1
SC 2
a
l1
l2
Vacuum
Hz
Q2
Q1
l1/a
An hypotesis:
Gap and Penetration depth depends on magnetic field

## Slide 10
Q2
Q1
b
5
10
15
20
25
30
35
40
45
50
QTot

## Slide 11
+
=
Q2
Q2e-k2b
Q1
b
Why Q increases with field?
The more l1 increases vs field
The more SC2 ( low losses) is involved

## Slide 12
+
=
b
Q1
Q2
a/l0
O
0.1
1
10
The ticker is SC 1, the smoother is the Q-rise

## Slide 13
One of our thermal diffused NbN

## Slide 14: Cu sputtering into Nb 6GHz cavity
Cathode
Cavity

## Slide 15
Sputtering of a Cu overlayer onto a Nb 6GHz cavity

## Slide 20
Didn’t you notice anything strange?

## Slide 21
Sputtering of a Cu overlayer onto a Nb 6GHz cavity

## Slide 23: Sketch of the furnace
Work head
15 KW
Power
supply
Pyrometer
Gas
bottle
Low overpressure
(250-3000)ºC
Exhaust gases
Coil
Input gas
Cavity or Sample

## Slide 25
We took a contaminated cavity, exposed to air for years and with a Q around 1e+6
We treated at 2000°C for only a few tenths of seconds at atmospheric pressure without using vacuum
The Q at 1,8 K jumped up for 3 orders of magnitede

## Slide 29: We did not act onto RRes. We acted onto RBCS!!!

## Slide 30: CONCLUSIONS
A new treatment of the of time of the minute, at temperatures over 2000°C, without using vacuum, allows the recovery of performances of 6 GHz cavities

## Slide 31
THANK YOU