## Slide 1
Nb films produced by Energetic Condensation via ECR
A-M Valente-Feliciano, J. Spradlin, L. Phillips, C. Reece, G. Eremeev, B. Xiao, X. Zhao, O. Trofimova (Jlab)
F. Stevie, D. Batchelor
(NCSU)
,

## Slide 2: OUTLINE
Motivation/Approach for SRF thin films development
Nb Films on Insulators
Nb Films on Copper
Concluding Remarks

## Slide 3: Superconducting RF Cavities
Breakdown fields close to the de-pairing limit of 50 MV/m for Nb. Best Nb cavities approaching their intrinsic limit at Hmax = HC
Nb has the highest Tc among all pure metals and the highest lower critical field Hc1≈170 mT (2K) among all superconductors . Meissner state can exist up to H = Hc.

## Slide 4: Thin Films: niobium –state of the art
RRRNb= R300K/R10K
CERN 2000
Bulk Nb
1.5 GHz Nb/Cu
1.5 GHz Nb/Cu cavities, sputtered w/ Kr @ 1.7 K (Q0=295/Rs)
LEP II
350MHz Nb/Cu (4.2K)
Gauge for mean free path & material quality, affected by scattering centers such as structural defects, impurities …
CERN LEP 2 272 x 353MHz Nb/Cu 4-cell cavities
INFN Legnaro 52 x 160 MHZ Nb/Cu QWR
1.5 GHz Nb/Cu cavities, sputtered w/ Kr @ 1.7 K (Q0=295/Rs)
Standard films
Oxide-free films
Courtesy: P. Jacob - EMPA
Columnar grains, size ~ 100 nm
In plane diffraction pattern: powder diagram
(110) fiber texture  substrate plane
Equi-axed grains, size ~ 1-5mm
In plane diffraction pattern: zone axis [110]
Heteroepitaxy
Nb (110) //Cu(010) , Nb (110) //Cu(111),Nb (100) //Cu(110)
RRRmax =28
RRRmax= 40

## Slide 5
Bulk-like performance Nb film
major system simplifications.
highest level of quality assurance and reliable performance.
Use of substrates with higher thermal conductivity
CERN 2000
Bulk Nb
1.5 GHz Nb/Cu
1.5 GHz Nb/Cu cavities, sputtered w/ Kr @ 1.7 K (Q0=295/Rs)
LEP II
350MHz Nb/Cu (4.2K)

## Slide 6: Tailoring for optimum RF performance
Careful characterization of the attained composition and microstructure
Close association with resulting rf surface impedance and superconducting properties
3 sequential phases for film growth
  Film nucleation on the substrate (Nb, Al2O3, Cu; single crystal & polycrystalline)
  Growth of an appropriate template for subsequent deposition of the final RF surface
  Deposition of the final surface optimized for minimum defect density.

## Slide 7: Deposition Techniques
Control over the deposition process is exercised by only
3 first-order vapor parameters & 1 first-order substrate parameter.
Vapor parameters Absolute arrival rates of film atoms
Partial pressures of background gases in the chamber Energies of the deposition fluxes.
Substrate parameter Substrate temperature T.
Without energetic atoms, only the substrate temperature influences the processes of physi- and chemisorption, thermal desorption, nucleation, nuclei dissociation, surface diffusion, and formation of specific nucleation sites.
However practical substrates for SRF cavities (Al, Cu) may not allow heating to high temperature!
Typical energy ranges for different PVD processes.
PIIID = plasma immersion ion implantation and deposition
IBAD = ion beam assisted deposition
PLD = pulsed laser deposition
VAD = vacuum arc deposition
IBA-MBE = ion beam assisted molecular beam epitaxy
MS = magnetron sputtering
MBE = molecular beam epitaxy.

## Slide 8: Energetic Condensation
The additional energy provided by fast particles arriving at a surface can induce the following changes to the film growth process:
Generalized Structure Zone Diagram
A. Anders, Thin Solid Films 518(2010) 4087
residual gases are desorbed from the substrate surface
chemical bonds may be broken and defects created thus affecting nucleation processes and film adhesion
film morphology changes
microstructure is altered
stress in the film alters
As a result of these fundamental changes, energetic condensation allows the possibility of controlling the following film properties:
  the density of the film may be modified to produce improved optical and corrosion-resistant coatings
  the film composition can be changed to produce a range of hard coatings and low friction surfaces
  crystal orientation may be controlled to give the possibility of low-temperature epitaxy

## Slide 9: Energetic Condensation via ECR
Niobium vapour produced by an e-beam gun is ionized by an ECR process. The Nb ions can be accelerated to the substrate by an appropriate bias. Energies in excess of 100 eV can be obtained.
Generation of plasma
3 essential components:
Neutral Nb vapor
RF power (@ 2.45GHz)
Static B  ERF with ECR condition
Why ECR?
No working gas
High vacuum ie. reduced impurities
Singly or “quasi-singly charged” ions
Controllable deposition energy
90° deposition flux
(Possible to help control the crystal structure)
Excellent bonding
No macro particles
Wu, G., et al.
J. Vac. Sci. Technol. A Vol. 21, No. 4, (2003)

## Slide 10
Energetic vacuum deposition by ECR plasma

## Slide 11: Samples produced on different substrates
Insulating:
    Al2O3 (11-20)
    Al2O3 (11-20)
    MgO(100)
    SrTiO3
Amorphous (Al2O3 , AlN), fused silica
Metallic:
  Cu (100)
  Cu (110)
  Cu (111)
  Fine grain Cu
  Large grain Cu
Typical vacuum during plasma in ECR system:<5x10-8 Torr
  Effect of interface quality :
  Substrate pre-treatment ex-situ & in-situ
Cu grain size and presence/absence of Cu oxide at interface
  Influence of energy of incoming ions : Bias voltage (0V, -150V)
  Influence of adatom mobility : Coating temperature

## Slide 12: Nb films grown on insulators
Less impurities than bulk Nb – SIMS data
The hydrogen content of ECR Nb films is found to be much lower than for the standard bulk Nb material as shown by the SIMS data.
XRD pole figures show the presence of growth domains (rotation the poles of 70°)
As the film grows one growth variant prevails.
Evolution of crystal structure with thickness

## Slide 13: Nb films grown on insulators
“Amorphous” Al2O3 ceramic
Crystalline Al2O3 (11-20)
ECR Nb films
Coated simultaneously
RRR= 247
RRR=89
A. R. Wildes et al., Thin Solid Films, 401 7 (2001)
Epitaxy of Nb on Al2O3 (11-20) , Al2O3 (0001), MgO (100), (110), (111)
Polycrystalline films with micron size grains grown on nano-crystalline/amorphous materials such Al2O3 and AlN ceramics and fused silica.

## Slide 14
Effect of Ion energy, baking & coating temperatures
on RRR
30’ coating, pressure during coating ~2.5e-8Torr, 360°C
Nb grown on (11-20) sapphire (Bias -120V)
RRR vs. .Bake & Coating Temp.
Nb grown on (11-20) sapphire
RRR vs. Bias
Nb films grown on insulators

## Slide 15
Effect of Ion energy: Template creation/subsequent growth
-180V+0V
Indication that once adequate template created, higher film quality can be achieved with subsequent growth at energies that promote epitaxy and less defects
Nb films grown on insulators

## Slide 16
Highest RRR measured for Nb/insulators
Substrate | RRR
Single crystal insulator | 
MgO (100) | 176
MgO (110) | 424
MgO (111) | 197
a-Al2O3 | 488
c-Al2O3 | 247
Amorphous | 
Al2O3 ceramic | 89
AlN ceramic | 72
Fused Silica | 34

## Slide 17: Nb on Cu single crystals
RRR=88
RRR=242
RRR=76
In the same run, Nb/fine grain Cu RRR=82
Nb/large grain Cu RRR=169

## Slide 18
{110} Nb
{200} Nb
{211} Nb
{110} Nb
{200} Nb
{211} Nb
ECR Nb (100) on Cu(110)
ECR Nb (110) on Cu(100)
{200} Nb
{211} Nb
{110} Nb
ECR Nb (110) on Cu(111)
Nb on Cu single crystals

## Slide 19
Nb films on polycrystalline Cu substrates
RRR=169
RRR=82
Nb/large grain Cu
(substrate heat treated ex-situ @ 1000°C, 12h)
Nb/fine grain Cu

## Slide 20
Nb/Cu – High Resolution TEM

## Slide 21
150 x 150 μm, 1 μm resolution, CI Avg. 0.71
120 x 150 μm, 1 μm resolution,
CI Avg. 0.23
50 x 75 μm, 1 μm resolution,
CI Avg. 0.16
Bias -120V, 2mm
Bias 0V , 4mm
Typical Cu substrate
Effect of Bias Voltage
Ab-normal growth
vith bias
vs.
columnar growth
without bias
Nb films on polycrystalline Cu substrates

## Slide 22
Nb films on Cu substrates - RRR
Single crystal Cu substrates
Cu (100)
Cu (110)

## Slide 23
Nb films on Cu substrates - RRR
Large grain Cu substrates
(Heat Treated @ 1000°c ex-situ)
Fine grain Cu substrates

## Slide 24
Nb films on Cu substrates
Substrate | RRR
Single crystal | 
Cu (100) | 129
Cu (110) | 275
Cu (111) | 242
Polycrystalline | 
Cu fine grains | 150
Cu large grains | 289
High RRR are also achieved on Cu substrates both mono-crystalline and polycrystalline.
Some dependence of RRR on the incident ion energy is observed. However, additional studies are necessary due to the strong influence of substrate crystalline quality on the resulting film structure. Similar high RRR values are achieved for both single crystal and polycrystalline substrates, suggesting that the presence of grain boundaries is not necessarily detrimental.

## Slide 25: RF Performance of ECR Nb films
One of the parameters of choice for evaluating SRF surfaces is the surface resistance below Tc.
A series of surface resistance measurements in a 7.5 GHz sapphire-loaded TE011 cavity [10] is under way for films coated simultaneously with those for which the RRR values are presented, both on polycrystalline Cu and single crystal sapphire substrates

## Slide 26
Niobium Films – towards cavity coating
A 2.8Gz half-cell was coated in the ECR chamber: The film thickness along the cell profile varies from 4mm (equator) to 6mm (iris) →conformality of the ECR process
Note: the substrate is very rough, was only grossly mechanically polished
Cut for thickness measurement
Location | Thickness [mm]
L1 | 3.804
L2 | 4.275
L3 | 4.200
L4 | 4.714
L5 | 5.136
L6 | 4.288
Location | Thickness [mm]
L1 | 6.189
L2 | 5.675
L3 | 6.081
L4 | 5.986
L5 | 6.015
L6 | 6.893

## Slide 27
Niobium Films – towards cavity coating
Concept for a cavity coating system based on energetic condensation (HiPIMS or ECR enhanced sputtering)
                Easily scalable for different cavity frequencies.
                A must for 200MHz muon cavities!
Gate valves
Cavity
Energetic condensation
Normal angle of incidence
→ better film structure
Source of ions in vacuum
Low gas pressure and use of Krypton
→ no gas inclusion →high RRR
No thermalization of the ions in transit
Bellow
Bias Grid
Nb cathode
Cavity
Nb cathode
Advantages
Kr injection
port

## Slide 28: SUMMARY
Nb films deposited by energetic condensation via ECR exhibit high crystalline quality:
  Film quality highly dependent on interface ( crystalline, amorphous…), substrate cleanliness
  Improved quality by in-situ pre-heating of substrates. Some substrate heating during coating seems necessary to improve RRR and reduce surface resistance around 2K.
  Unprecedented film quality due to energetic ions across all substrates.
  Exploration of zones in Structure Zone model never achieved before
  Some dependence observed as a function of ion arrival energy for sapphire, magnesium oxide and copper substrates.
  Indication that good quality substrate can be created for subsequent growth at energies that promote epitaxy and generate less defects.
Nb films with unprecedented RRR values (equivalent to bulk niobium) have been produced.
The investigation of the surface impedance as a function of the coating parameters and superconducting characteristics of the films is under way.
Preparation for cavity coating in 2013

## Slide 29: SRF Thin Films Collaboration
Under DOE HEP Grant ARRA & U.S. DOE Contract No. DE-AC05-06OR23177
Jlab: C.Reece, A-M Valente-Feliciano, J. Spradlin, L. Phillips, X. Zhao, B. Xiao, A. Wu
W&M: A. Lukaszew, D. Beringer, W. Roach, C. Clavero , R. Outlaw, O. Trofimova
NSU: Q. Yang
ODU: H. Baumgart, D. Gu
Black Labs LLC: R. Crooks
NCSU: F. Stevie, D. Batchelor