## Slide 1: Magnetic Flux Structure at Different Fields in Cavity Niobium by Bitter Decoration
F. Barkov, A. Romanenko

## Slide 2: Motivation
Magnetic flux penetration is a possible candidate for losses in SRF cavities
No high resolution studies of magnetic flux entry into cut-out samples were produced before
Bitter decoration technique allows to investigate magnetic field distribution with a “single-vortex” spatial resolution
The main idea was to directly observe spatial variations of surface superconducting properties

## Slide 3: Experimental technique
1 – Helium cryostat; 2 – Insert with decoration chamber (A); 3 – Plug/socket combination; 4 – Evaporator; 5 - Sample; 6 – Protective screen; 7 – Thermometer; 8 – Mechanical valve; 9 -Solenoid
1. Superparamagnetic nanoparticles are deposited to mark regions with magnetic field
2. Scanning electron microscope is used to examine particles distribution
This is how the first direct observation of the vortex lattice was obtained!
U. Essman and H. Trauble,
Physics Letters 24A, 526 (1967)

## Slide 4: Experimental parameters
Cut-outs from cavities:
-hot spots
-120C baked spots
Mechanically polished + 800C baked
Mechanically polished + 800C baked+ 20 microns EP
Mechanically polished + 800C baked + 20 microns BCP
T=1.7->5..6 K
H=0..120 mT
Samples

## Slide 5: Field Cooling Results
H=10 mT. Hot spot. Flux bundles are observed instead of individual Abrikosov vortices.
Hot Spot

## Slide 6
H=10 mT. Hot spot. Zoom-in from previous picture. Average number of magnetic flux quanta per bundle is ~80
flux bundles
Meissner regions
Hot Spot

## Slide 7
H=10 mT. Hot spot. No single vortices are resolved even at highest magnification
Hot Spot

## Slide 8
H=10 mT. Baked spot. No vortices, just flux bundles.
Meissner regions
flux bundles
Baked Spot

## Slide 9
H=32 mT. Hot spot. Flux regions now form a “connected” structure
Hot Spot

## Slide 10
H=32mT. Hot spot. Zoom-in from previous picture
Hot Spot

## Slide 11
H=32 mT. Hot spot. High-magnification image. No single vortices are resolved
Hot Spot

## Slide 12
H=60 mT. Hot spot.
Hot Spot

## Slide 13
H=60 mT. Hot spot. Zoom-in from white spot from previous picture. Individual vortices are observed. Inset: Fast Fourier Transform pattern with 6 maxima corresponding to a long range ordered hexagonal lattice
B=76±5 mT
Hot Spot

## Slide 14
H=80 mT. Hot spot. Vortex lattice is everywhere, there are no Meissner regions.
Hot Spot

## Slide 15
H=60 mT. Baked spot. The topology of Meissner regions is different.
Baked Spot

## Slide 16
H=60 mT. Baked spot. Zoom-in from previous picture.
B=74±5 mT
Baked spot

## Slide 17: Results for flat samples
H=8 mT. BCP sample
flux bundles
Abrikosov vortices
Flat sample

## Slide 18
H =8 mT. BCP sample. Coexistence of Abrikosov vortices and Shubnikov domains.
region with Abrikosov vortices
flux bundles
Flat sample

## Slide 19
H=8 mT. BCP sample. Vortices do not form ordered lattice. FFT pattern is a circle.
Flat sample

## Slide 20: Zero Field Cooling Results
We did not observe penetration of magnetic field into samples up to:
  60 mT for baked spot
  120 mT for hot spot

## Slide 21: Summary
We have investigated how magnetic field penetrates into cavity cutouts and flat niobium samples
Cavity grade niobium is “type 1.5” superconductor
  Coexistence of regions with Abrikosov vortices and flux bundles is observed for flat samples
  Field driven transition from type-I to type-II superconductivity is observed for cavity cutouts
Hot and baked spots behave similarly
Pinning plays a significant role and prevents vortices penetration from the sample edges in ZFC regime

## Slide 22: Acknowledgments
Marianne Bossert, Rob Schuessler, Donna Hicks, FNAL – samples preparation
Prof. L.Ya.Vinnikov and Prof. V.V. Ryazanov, ISSP RAS – help with the experiments, useful discussions