## Slide 1: State of the Art and Future Potential of Nb/Cu Coatings
Sergio Calatroni, Giovanni Terenziani, and all CERN SRF community

## Slide 2: Niobium Magnetron Sputtering
Sputtering parameters (1.5 GHz):
  Sputter gas pressure of 1.5x10-3 mbar (Ar or Kr)
  Plasma current stabilized at 3A - DC
  Sputter potential ~ -360 V
  Coating temperature is 150 °C.
  Thickness: 1.5 µm
“Standard films”:
  RRR: 11.5 ± 0.1
  Argon content: 435 ± 70 ppm
  Grain size: 110 ± 20 nm
  Tc: 9.51 ± 0.01 K
  Strain: a/a  = 0.636 ± 0.096 %
-V

## Slide 3: Diode sputtering

## Slide 4: Coating of beta = 1 and lower beta cavities
288 Nb/Cu cavities installed in LEP
16 Nb/Cu cavities installed in LHC
About 300 coatings on 1.5 GHz for R&D
Low-beta studies, several 10’s of coatings
(+ Soleil prototypes, 3HC, 200 MHz Cornell...)
HIE-ISOLDE about 10 coatings

## Slide 5: LNL
56 cavities total
A.M. Porcellato

## Slide 6: Cost advantages
Cu OFE sheets: 10 EUR/kg
Nb RRR 300 sheets: 500 EUR/kg
Simpler cryostats (stainless steel), no magnetic shielding
Conduction cooling is possible
Cost of LEP200 RF cryomodules was about half of what it would have been if using cavities of bulk Nb (E. Chiaveri)

## Slide 7: Quenches don’t happen
Joachim Tuckmantel - Thermal effects in superconducting RF cavities: some new results from an improved program
CERN-EF-RF-84-6. - 1984.
100 micron radius steel defect
Nb: 10.2 K
Nb/Cu: 3.3 K
Nb bulk
Nb / Cu

## Slide 8: Effect of external magnetic field
Losses due to trapped external magnetic field at 1.7 K are characterized as
Rfl = (Rfl0 + Rfl1 HRF) Hext
The minimum values are obtained using krypton as sputter gas:
Rfl0 = 3n/G Rfl1 = 0.4 n/G/mT
Coatings on oxide-free copper
Coatings on oxidized copper
1
10
10
100
1+0/2
Rfl0[n/G]
(a)
1
10
1
10
Rfl1[n/G/mT]
1+0/2
(b)
Rfl (HRF, Hext, T) has a dependence on  similar to RBCS(0,T), but the physical mechanism must be different
bulk Nb
bulk Nb
Coatings on oxide-free copper
Coatings on oxidized copper

## Slide 9: Mechanical stability
No dynamic tuning needed

## Slide 10: BCS resistance at zero RF field
RBCS at 4.2 K
(1.5 GHz)
Nb bulk: ~900 n
Nb films: ~400 n
RBCS at 1.7 K
(1.5 GHz)
Nb bulk: ~2.5 n
Nb films: ~1.5 n
1
10
350
400
450
500
550
600
650
700
750
800
850
900
2
5
20
RBCS (4.2K) [n]
1+0/2
Nb bulk
Curve: theoretical
The dependence of RBCS (0,T) on  was known theoretically and has been verified by changing the sputter gas

## Slide 11: State-of-the-art at 1500 MHz – 1.7 K – single cell
Q = 1x1010 @ 15 MV/m
Q = 3x109 @ 20 MV/m
0 45 90
Hsurf [mT]
Q = 1x1010 @ 15 MV/m is a value that would make film cavities a competitive option for proton accelerators

## Slide 12: TEM view – film defects
Crystallographic defects can be at the origin of reduced Hc1 compared to bulk Nb
~100 nm
RRR of films: 10  30

mfp of films 30  100 nm
Grain size of films > 100 nm

RRR limited by intragrain defects in most cases
A defect cluster has a different effect on resistivity and flux trapping

## Slide 13: Measurement of Hc1
SC coil at the outer wall of the cavity at equator Hext up to 2T over 3 cm2
Hpenetration films  0.6 Hpenetration bulk

## Slide 14: Structure zone model from A. Anders
Based on “Structure Zone Model” - Thornton, J.Vac. Sci. Technol. 11 (1974) 666

## Slide 16: State of the art
Bulk Nb
1.5 GHz Nb/Cu
1.5 GHz Nb/Cu cavities, sputtered w/ Kr @ 1.7 K (Q0=295/Rs)
LEP II
350MHz Nb/Cu (4.2K)
CERN 2000

## Slide 17: Angle of incidence of the coating
Average angle of incidence increases
There is a “threshold” effect

## Slide 18: Film analyses
Standard films
Oxide-free films
0.5 µm
0.5 µm
FIB cross sections courtesy: P. Jacob - EMPA
 | Standard | Oxide-free
RRR | 11.5 ± 0.1 | 28.9 ± 0.9
TC | 9.51 ± 0.01 K | 9.36 ± 0.04 K
Ar cont. | 435 ± 70 ppm | 286 ± 43 ppm
Texture | -110 | (110), (211), (200)
Hc1 | 85 ± 3 mT | 31 ± 5 mT
Hc2 | 1.150 ± 0.1 T | 0.73 ± 0.05 T
a0 | 3.3240(10)Å | 3.3184(6) Å
a/a | 0.636 ± 0.096 % | 0.466 ± 0.093 %
Stress | -706 ± 56 MPa | -565 ± 78 MPa
Grain size | 110 ± 20 nm | > 1 µm

## Slide 19: Measurements of Hc1 on Nb films
Magnetic moment with squid magnetometer filed parallel to the sample
HC1 = 52.5  2 mT
Same film, trapped magnetic moment with squid magnetometer
(fit with V.V. Moshchalkov et al., Physica C 175 (1991) 407)
HC1 = 31  3 mT

## Slide 20: TEM micrographs in plan view
Grain size ~ 100 nm
Fibre texture
Diffraction pattern:
powder diagram
Standard
Oxide-free
Grain size ~ 1-5mm
Heteroepitaxy
Diffraction pattern:
zone axis [110]
500nm
500nm

## Slide 21: TEM micrographs in cross section
(110) fibre texture
 substrate plane
Standard
Oxide-free
Heteroepitaxy
Nb (110) // Cu(010)
Nb (110) // Cu(111)
Nb (100) // Cu(110)
500nm
500nm