## Slide 1: Production status of high-purity Nb sheets for European XFEL and FRIB projects - Based on current production of Nb sheets for European XFEL and FRIB projects
Hiroaki Umezawa
CTO
Tokyo Denkai Co., Ltd.
07 November, 2012

## Slide 2: Agenda
High-purity Nb sheet production for European XFEL project
High-purity Nb sheet production for FRIB project

## Slide 3
High-purity Nb sheet production for European XFEL project
High-purity Nb sheet production for FRIB project

## Slide 5: Nb for Euro XFEL Project
Tokyo Denkai tendered an offer for 5,886 high-purity Nb sheets of 265 mm x 265 mm x 2.8 mm.
This quantity is as 50% of half cell material of SC cavity of the European XFEL project .
We won the bid and our offer was completely accepted.

## Slide 6: Shipping schedule
We received the official order on January 7, 2011.

## Slide 7: Shipping schedule
We received the additional order on October 3, 2011.
Notes: 7

## Slide 8: Production rate
Average production speed: 4,000sheets/year

## Slide 9: Investment for new equipments
To reduce Nb sheet production time, we installed two new types of machines.
  Automatic Buffing (polishing) Machine
    For final sheets
    For thick sheets
  Automatic Etching Machine

## Slide 10: Automatic buffing machine (ABM)

## Slide 11: Automatic Etching Machine (AEM)

## Slide 12
High-purity Nb sheet production for European XFEL project
High-purity Nb sheet production for FRIB project

## Slide 13: Difference between Nb sheet for XFEL and FRIB
RRR
  Euro-XFEL: RRR>300
  FRIB: RRR>250
Sheet size
  Euro-XFEL: 2.8 mm x 265 mm x 265 mm, 1.7kg
  FRIB: Eight different sheet size

## Slide 14: Difference between Nb sheet for XFEL and FRIB
3x620x620mm
9.9kg
4x600x600mm
12.4kg
4x500x500mm
8.6kg
3x520x520mm
7.0kg
3x450x560mm
6.5kg
2x520x520mm
4.7kg
3x330x330mm
2.8kg
1.25x400x400mm
1.7kg
2.8x265x265mm
1.7kg
1.3GHz

## Slide 16: Automatic Etching Machine 2
Maximum sheet size:
900 mm x 1,700 mm

## Slide 18: Summary
Production of 5,886 Nb sheets (10tons) for the E-XFEL project was achieved last week.
Delivery time was earlier than the scheduled time.
Average production rate was approximately 4,000 sheets/year.
Delivery of additional 1,484 Nb sheets (2.5 tons) is scheduled for Feb and June 2013.
This 7,370 sheets production boost our confidence in the mass production of high-purity Nb sheets.

## Slide 19: Summary
Difficulty in production of Nb sheets for the FRIB project was the required sheet size.
Etching of big sheets exposed workers to danger.
Installation of a new etching machine for big sheets solved the problem.
The new machine is operating well, freeing workers from dangerous tasks.
The first delivery to FRIB was achieved last month.

## Slide 20
Thank you for your attention.